## Slide 1: Biomass pelletization for energy and biorefinery use
Benjamin RABDEAU
RAGT Energie
B4A Final Conference/BLP 2025,
28-30 January, Montpellier

## Slide 2: Purpose of biomass densification
Under-exploited agricultural by-product often have physical properties not adapted to their final use:
  High moisture content / not stabilized
  Low bulk density
  Inadequate particle size
  Not homogenous
The densification of these biomasses can alleviate these obstacles

## Slide 3: Principle
Dense
Homogenous
Pelletizing
Pellet
Pre-treatment
Biomass
Clean fuel (energy/cooking)
Animal feeding production
Soil amendment production

## Slide 4: General pelletizing process
Biomass
Shredding
Drying
Grinding
Mixing
Pelletizing
Cooling
Pellets
Pretreatment : optional steps that depend for each biomass
Adaptation of pelletizing parameters are crucial :
Moisture content before pelletizing
Compression ratio of the pellet die

## Slide 5: Main pellet mill technologies
Ring-die
Flat-die

## Slide 6: Pilot scale equipment for adaptation trials

## Slide 7: Pelletization inputs and outputs
[BD] Bulk density
[DU] Mechanical durability
[M] Moisture content
[D L] Diameter / Length
Die temperature
Energy consumed
Fines produced
Production flow rate
[MC]
Moisture content
[CR]
Compression ratio
Pretreatment
Chemical properties
Physical properties
INPUT Biomasses
INPUT Variable parameters
OUTPUT Pellet quality
OUTPUT Production
PELLET PRODUCTION

## Slide 8: Iterative trials to improve pellet quality
Photos of different pellets produced with peanut shells |  |  |  | 
Moisture content | 12% | 16% | 14% | 16%
Compression ratio | 5 | 5 | 9 | 8
Fines (lower is better) | 40% | 25% | 10% | 6%
Mechanical durability (higher is better) | 43% | 83,7% | 81,3% | 95,5%
Bulk density (600-750 kg/m3) | 588 kg/m3 | 675 kg/m3 | 680 kg/m3 | 696 kg/m3
Pellet production performance and pellet physical properties improve at each step

## Slide 9: Adaptation of pelletizing parameters
Moisture content
12%
13%
14%
15%
16%
6
12
Palm seed shells
Peanut shells
Millet stalks
Cocoa pods
8
10
Each biomass behaves differently during pelletizing :
Need more or less water
Need more or less compression
Compression ratio
= e/d
e : length of compression canal
d : diameter of compression canal
Notes: Changer emplacement des noms et photos

## Slide 10: Best operating conditions on some biomasses
Photos of the best pellets obtained for four biomasses |  |  |  | 
Biomass | Palm seed shells | Peanut shells | Millet stalks | Cocoa pods
Moisture content | 12% | 16% | 13,5% | 14%
Compression ratio | 12 | 8 | 6,5 | 10
Mechanical durability (higher is better) | 88,1% | 95,5% | 98,8% | 99,2%
Bulk density (600-750 kg/m3) | 733 kg/m3 | 696 kg/m3 | 703 kg/m3 | 741 kg/m3
Promising results
Adequate pellet quality with different conditions

## Slide 11: Difficulties of animal feed pellet production
Chart: 
| 0 < P ≤ 0,2 | 0,2 < P ≤ 0,5 | 0,5 < P ≤ 1 | 1 < P ≤ 2 | 2 < P ≤ 3,15 | 3,15 < P ≤ 8 | 8 < P
% fraction | 0.80503 | 22.2974 | 23.3326 | 45.4947 | 5.8384 | 1.9361 | 0.29577
∑fraction | 0.80503 | 23.1024 | 46.435 | 91.9297 | 97.7681 | 99.7042 | 100
Chart: 
| 0 < P ≤ 0,2 | 0,2 < P ≤ 0,5 | 0,5 < P ≤ 1 | 1 < P ≤ 2 | 2 < P ≤ 3,15 | 3,15 < P ≤ 8 | 8 < P
% fraction | 13.655 | 16.8738 | 31.7903 | 33.424 | 0.56057 | 3.3112 | 0.38517
∑fraction | 13.655 | 30.5288 | 62.319 | 95.7431 | 96.3036 | 99.6148 | 100
Chart: 
| 0 < P ≤ 0,2 | 0,2 < P ≤ 0,5 | 0,5 < P ≤ 1 | 1 < P ≤ 2 | 2 < P ≤ 3,15 | 3,15 < P ≤ 8 | 8 < P
% fraction | 13.9432 | 33.7265 | 36.9184 | 12.0215 | 0.23251 | 3.0341 | 0.12375
∑fraction | 13.9432 | 47.6697 | 84.5881 | 96.6097 | 96.8422 | 99.8763 | 100
Chart: 
| 0 < P ≤ 0,2 | 0,2 < P ≤ 0,5 | 0,5 < P ≤ 1 | 1 < P ≤ 2 | 2 < P ≤ 3,15 | 3,15 < P ≤ 8 | 8 < P
% fraction | 15.6681 | 16.7844 | 26.2479 | 36.3856 | 1.085 | 3.6113 | 0.2177
∑fraction | 15.6681 | 32.4525 | 58.7004 | 95.086 | 96.171 | 99.7823 | 100
Chart: 
| 0 < P ≤ 0,2 | 0,2 < P ≤ 0,5 | 0,5 < P ≤ 1 | 1 < P ≤ 2 | 2 < P ≤ 3,15 | 3,15 < P ≤ 8 | 8 < P ≤ VB
% fraction | 1.5223 | 22.1987 | 62.6833 | 13.5231 | 0.040766 | 0.03571 | -0.0037922
∑fraction | 1.5223 | 23.721 | 86.4042 | 99.9273 | 99.9681 | 100.0038 | 100
Chart: Bulk density (kg/m3) of grinded biomasses and starch
Palm seed shells | 582.822
Millet stalks | 177.07
Peanut shells | 389.92
Cocoa pods | 328.97
Starch | 543.88
Palm seed shells
Millet stalks
Peanut shells
Cocoa pods
Starch
Each of these ingredients has its own :
  Particle size
  Density

## Slide 12: Difficulties of animal feed pellet production
From one biomass to a recipe/blend of multiple ingredients :
  Different pre-treated biomasses
  Protein concentrate from biorefinery
  Other
Each of these ingredients has its own :
  Particle size
  Density
→ It increases the challenge to produce good quality pellets

## Slide 13: Outlook : Biochar pellet production
Rice husk biochar
Peanut shells biochar
Biochar pellets
Need higher moisture content (25-35%)
Need binder (5-15%)