## Slide 1: Up-grading agro-wastes from western Africa in biocomposites applications
Souha MANSOUR, Amandine VIRETTO, Marie-France THEVENON & Loïc BRANCHERIAU
CIRAD
B4A Final Conference/BLP 2025,
28-30 January, Montpellier

## Slide 2: GENERAL OVERVIEW
QUANTITIES PRODUCED IN AFRICA IN 2020
TYPHA
MILLET STALKS
RICE HUSK
COCOA PODS
OIL PALM EMPTY FRUIT BUNCH
300,000 to 500,000 tons
26.31 million tons
8.71 million tons
1.33 million tons
23.6 million tons
Notes: TPY extracted from Senegal’s river

## Slide 3: GENERAL OVERVIEW

## Slide 4: MATERIALS AND PARAMETERS
TYPHA
RICE HUSK
COCOA PODS
MILLET STALKS
OIL PALM EMPTY FRUIT BUNCH (OPEFB)
BIOMASS
Melamine-Urea-Formaldehyde (MUF)
BINDER
Application in the housing sector
Non-load-bearing applications
Resistant to the tropical climate
PANELS
BIOMASS
FIBER/BINDER RATIO
GRANULOMETRY
PARAMETERS

## Slide 5: FIBERS PREPARATION
Biomass dried at 80 °C for 24h
Grinding with a sieve of 6 mm
Lignocellulosic fibers
5

## Slide 6
1
CHEMICAL COMPOSITION
Chart: 
| Typha | Rice Husk | Millet Stalks | OPEFB | Cocoa Pods
Hemicelluloses | 21.6482 | 19.3503 | 24.731 | 23.5335 | 9.4418
Cellulose | 40.9148 | 40.2284 | 48.6537 | 39.4909 | 27.8996
Lignin | 17.1428 | 17.3182 | 11.5122 | 17.1325 | 30.2984
Ash | 0.42648 | 4.5447 | 0.32337 | 1.2892 | 0.35711
Others | 19.8677 | 18.5584 | 14.7797 | 18.5539 | 32.0031
FIBERS CHARACTERIZATION
6
Notes: The biomasses all present similar quantities of the main constituents, except for the cocoa pods which have more lignin than all the others.
Rice husk is also special among the rest of the biomasses due to its high ash quantity which is caused by the presence of Silica

## Slide 7
1
CHEMICAL COMPOSITION
BIOMASS | RESIDUE (%) | DEGRADATION TEMPERATURE (°C)
Cocoa | 32.4 ± 1.1 | 317.2 ± 3.5
Millet | 25.9 ± 1.0 | 316.7 ± 4.1
OPEFB | 25.9 ± 1.0 | 317.7 ± 4.7
Rice | 34.0 ± 1.4 | 347.9 ± 1.5
Typha | 23.8 ± 1.8 | 333.1 ± 4.1
30 °C to 800 °C
10 °C.min-1
Nitrogen atmosphere
2
THERMAL STABILITY
FIBERS CHARACTERIZATION
7
Notes: Rice is the most stable with the highest residue % and that is predicted due to its high Silica content.

## Slide 8
1
CHEMICAL COMPOSITION
2
THERMAL STABILITY
MILLET STALKS
RICE HUSK
COCOA PODS
OPEFB
TYPHA
Optical microscope (x8)
3
SHAPE AND SIZE
FIBERS CHARACTERIZATION
8
Notes: An optical microscope was used to obtain an image of each biomass to understand more the structure of these materials.
OPEFB, Typha, and millet stalks all have an elongated fiber shape, unlike the cocoa pods that is more spherical.
As for the rice, its structure wasn’t affected by the grinding.

## Slide 9
1
CHEMICAL COMPOSITION
2
THERMAL STABILITY
3
SHAPE AND SIZE
FIBERS CHARACTERIZATION
Biomass | Apparent Density (kg/m3) | Real Density (kg/m3) | Porosity (%)
Cocoa | 484.7 | 1401.2 ± 8 | 65.4
Millet | 93.6 | 1229.8 ± 4.5 | 92.4
OPEFB | 157.1 | 1282.9 ± 3.0 | 87.8
Rice | 150.7 | 1482.9 ± 5.6 | 89.8
Typha | 65.9 | 1325.9 ± 1.3 | 95.0
4
DENSITY
9
Notes: Two tests were realized to measure the density.
At first a compaction test to measure the apparent density, then there’s the pycnometer to measure the real density.
Cocoa pods are the most dense. With high values of porosity for typha and millet stalks which previews an isolation behavior of the panels prepared with these two fibers.
Compaction has no std deviation

## Slide 10
1
CHEMICAL COMPOSITION
2
THERMAL STABILITY
3
SHAPE AND SIZE
4
DENSITY
5
DURABILITY
TOWARDS
TERMITES
FIBERS CHARACTERIZATION
Biomass | Termites activity
Rice | Activity decreases over time, no visible activity after 28 days
OPEFB | 3/5 no activity after 28 days 2/5 active termites
Millet | Termites actives
Typha | 2/5 activity decreases after 20 days 3/5 no activity after 20 days
Cocoa | 2/5 active termites 2/5 reduced activity after 28 days 1/5 no activity after 28 days
Pine Sapwood Control | The termites were very active during the test period Survival rate > 50%, The screening test is validated
27°C, RH > 75%
5 Weeks
Reticulitermes flavipes
10
Notes: The durability against termites was tested. The screening test was validated by the pine sapwood control.
Termites are most active with millet stalks due to the high cellulose/hemicellulose contents which constitutes a main food source for termites.
On the other hand, rice husk is the most resilient due to its silica content which is not a food source for termites

## Slide 11
1
CHEMICAL COMPOSITION
2
THERMAL STABILITY
3
SHAPE AND SIZE
4
DENSITY
5
COLOR
6
GRANULOMETRY
FIBERS CHARACTERIZATION
Chart: Sieve diameter (mm)
| 5 | 4 | 3.15 | 2.5 | 2 | 1.6 | 1.4 | 1 | 0.85 | 0.71 | 0.6 | 0.5 | 0.4 | 0.3 | 0.2 | 0.1 | < 0,1 / Fond
Typha | 5.4411 | 1.9317 | 4.3142 | 9.7875 | 11.5261 | 17.3213 | 10.2061 | 6.6001 | 2.4791 | 2.8332 | 14.7457 | 3.5093 | 2.1249 | 2.2215 | 3.4127 | 0.7727 | 0.7727
RICE | 0 | 0 | 0 | 1.8049 | 4.9288 | 48.0909 | 4.7726 | 16.9906 | 7.8271 | 7.8445 | 1.1281 | 1.2669 | 1.3363 | 2.395 | 0.81569 | 0.53801 | 0.22562
COCOA | 0.018619 | 0.8006 | 7.7825 | 19.8659 | 18.544 | 13.908 | 7.9129 | 6.9075 | 2.2715 | 3.5561 | 2.0853 | 2.1597 | 1.6943 | 3.221 | 2.8673 | 3.7796 | 2.6252
MILLET | 7.3467 | 1.1665 | 2.209 | 5.9568 | 11.7399 | 23.2812 | 9.4068 | 13.378 | 1.3155 | 6.7262 | 2.1842 | 2.8047 | 2.1593 | 3.3755 | 5.7334 | 0.6205 | 0.59568
OPEFB | 1.8367 | 0.29164 | 0.55225 | 1.4892 | 2.935 | 5.8203 | 2.3517 | 3.3445 | 0.32887 | 1.6816 | 0.54604 | 0.70117 | 0.53984 | 0.84388 | 1.4334 | 0.15513 | 0.14892
TYPHA
11
Notes: Finally, the granulometry distribution was measured.
Cocoa pods are centered around 2.5 mm and the rest is at 1.6 mm
The sieve used for the grinding process is 6 mm which is higher than the rice husk’s original size, therefore it is not very affected.

## Slide 12: PANELS PRODUCTION
120 °C
10 minutes
Cooling and demolding
Biomass
Melamine urea formaldehyde
1.76
kg
12
Notes: A mix of 1.76 kg total of biomass and binder was prepared then placed in a mold that was then pressed in a thermal press for 10 mins at 120 °C. and after cooling and demolding we obtained the different panels obtained as the photo shows
These panels will be compared to commercial particle boards

## Slide 13: PANELS FABRICATED
In Total:
25 panels with 3x5 replicates for rice
13
Fiber/Binder Ratio | BIOMASS |  |  |  | 
 | COCOA | RICE | OPEFB | MILLET | TYPHA
50/50 | Not tested | Not tested | The glue is difficult to dispense | Not tested | Too much powder surrounding the glue
60/40 | Easy mixing between components Glue is well distributed | Easy mixing between components Glue is well distributed | Difficulty dispensing glue Poor glue absorption | Too much powder surrounding the glue | Too bulky with little glue
70/30 | Easy mixing between components Glue is well distributed | Easy mixing between components Glue is well distributed | Too little glue, mixing was too difficult | Too bulky with little glue | Not tested
80/20 | Mixing more difficult due to the quantity of glue | No glue at the edge Difficult to distribute the glue | Not tested | Not tested | Not tested
Notes: One panel was fabricated for each fiber/binder ratio except for rice where five replicas were made for each.
The fiber/binder ratios were chosen depending on the biomass and the compatibility between the biomass and the binder.
The hardest mix was that of OPEFB, millet, and typha where the binder wasn’t easily distributed and it coagulated causing non-homogeneous distribution of the binder

## Slide 14: PANEL CHARACTERIZATION
1
APPARENT
DENSITY
Chart: 
| Rice | Typha | Palm | Millet | Cocoa | Reference
50/50 | 731.5 | 820.1 | 647
60/40 | 762.2 | 571.6 | 806 | 747.7 | 835.4
70/30 | 747.6 | 743.6 | 621.4 | 740.1
80/20 | 610.8 | 656.7
RICE
TYPHA
OPEFB
MILLET
COCOA
REF
Apparent Density (kg/m3)
14
Notes: The apparent density was measured showing that C60/40 are the most dense
With higher fiber content the density decreases
*MUF density 1300 kg per cubic meter

## Slide 15: PANEL CHARACTERIZATION
1
REAL
DENSITY
2
REAL DENSITY
Chart: Real Density (kg/m3)
| RICE | TYPHA | OPEFB | MILLET | COCOA | REF
50/50 | 0 | 1241.1857 | 1300.6889 | 0 | 0 | 1223.5333
60/40 | 1326.9556 | 1237.925 | 1159.3333 | 1235.15 | 1189.6111
70/30 | 1469.1444 | 0 | 1368.5778 | 1411.9 | 1333.9667
80/20 | 1505.9667 | 0 | 0 | 0 | 1327.1
15
Notes: Using a pycnometer we measured the real density in order to calculate the porosity

## Slide 16: PANEL CHARACTERIZATION
1
REAL
DENSITY
2
REAL DENSITY
3
POROSITY
Chart: POROSITY (%)
| RICE | TYPHA | OPEFB | MILLET | COCOA | REF
50/50 | 0 | 41.0671 | 36.9488 | 0 | 0 | 47.1204
60/40 | 42.5638 | 53.826 | 30.4744 | 39.4621 | 29.7782
70/30 | 49.1137 | 0 | 45.6662 | 55.9907 | 44.5211
80/20 | 59.4435 | 0 | 0 | 0 | 50.5137
16
Notes: The higher the fiber content the higher the porosity

## Slide 17: PANEL CHARACTERIZATION
1
REAL
DENSITY
2
REAL DENSITY
3
POROSITY
4
YOUNG’S
MODULUS
Chart: Young’s Modulus (MPa)
| RICE | TYPHA | OPEFB | MILLET | COCOA | REF
50/50 | 0 | 2852 | 2225.3333 | 0 | 0 | 3476.3333
60/40 | 2961 | 1232 | 3205 | 3962.3333 | 1750.6667
70/30 | 2561.4 | 0 | 1702.3333 | 2181 | 2141
80/20 | 997.4 | 0 | 0 | 0 | 890.6667
176
Notes: Using BING method we measured the young’s modulus
Millet showed higher values even higher than the reference panel
At 20% binder content the panels showed very low values of young’s modulus

## Slide 18: PANEL CHARACTERIZATION
1
REAL
DENSITY
2
REAL DENSITY
3
POROSITY
4
Chart: Fréquence (Hz)
| 150 | 200 | 250 | 315 | 400 | 500 | 630 | 800 | 1000 | 1250 | 1600 | 2000 | 150
OPEFB | 0.923 | 0.929 | 0.876 | 0.89 | 0.859 | 0.821 | 0.773 | 0.688 | 0.669 | 0.616 | 0.591 | 0.439
COCOA | 0.964 | 0.946 | 0.94 | 0.897 | 0.901 | 0.859 | 0.789 | 0.742 | 0.689 | 0.654 | 0.607 | 0.465
TYPHA | 0.88 | 0.884 | 0.835 | 0.867 | 0.843 | 0.751 | 0.696 | 0.647 | 0.604 | 0.586 | 0.543 | 0.372
MILLET | 0.784 | 0.839 | 0.73 | 0.739 | 0.716 | 0.708 | 0.686 | 0.61 | 0.51 | 0.534 | 0.494 | 0.297
RICE | 0.913 | 0.891 | 0.875 | 0.843 | 0.832 | 0.832 | 0.775 | 0.647 | 0.614 | 0.566 | 0.571 | 0.354
Chart: Fréquence (Hz)
| 150 | 200 | 250 | 315 | 400 | 500 | 630 | 800 | 1000 | 1250 | 1600 | 2000 | 150
P | 32 | 32.35 | 29.83 | 30.91 | 33.43 | 31.81 | 32.78 | 33.51 | 32.92 | 33.35 | 32.77 | 32.43
C | 26.02 | 26.66 | 28.21 | 26.74 | 28.08 | 26.74 | 27.86 | 28.44 | 27.94 | 27.57 | 27.91 | 28.91
T | 31.51 | 30.47 | 30.94 | 32.73 | 33.2 | 32.61 | 33.25 | 33.79 | 33.34 | 33.45 | 33.96 | 32.15
M | 31.31 | 32.69 | 33.63 | 30.16 | 31.43 | 32.19 | 33.29 | 33.87 | 33.28 | 33.59 | 33.72 | 32
R | 31.09 | 32.88 | 33.55 | 29.64 | 32.31 | 32.09 | 32.55 | 33.59 | 33.12 | 34.06 | 29.69 | 32.36
18
5
ACOUSTIC
ISOLATION
Notes: Absorption is not really affected by the fiber content (going from 60 to 80 didn’t change it much)
Cocoa has highest absorption
Millet, Typha, and OPEFB are the most soundproofing panels
Rice and cocoa with higher filler loading had lower values of transmission loss meaning the panels are less insulating

## Slide 19: PANEL CHARACTERIZATION
1
REAL
DENSITY
2
REAL DENSITY
3
POROSITY
4
ACOUSTIC
ISOLATION
5
YOUNG’S
MODULUS
Chart: Thermal conductivity (W/m.K)
| RICE | TYPHA | OPEFB | MILLET | COCOA | REF
50/50 | 0 | 0.175 | 0.214 | 0 | 0 | 0.2
60/40 | 0.185 | 0.132 | 0.152 | 0.236 | 0.148
70/30 | 0.199 | 0 | 0.179 | 0.176 | 0.162
80/20 | 0.15 | 0 | 0 | 0 | 0.144
6
THERMAL
CONDUCTIVITY
19
0.2
Notes: All panels are thermal insulators except OPEFB 50/50 AND M 60/40

## Slide 20: CONCLUSIONS
20
The five biomasses can be used
as reinforcing fibers in biocomposite panels
C 60/40 panels are the most dense
In terms of density
T 60/40 panels are the least dense
In terms of porosity
R 80/20, T 60/40, and M 70/30 panels are the most porous
C 60/40 and OPEFB 60/40 panels are the least porous
In terms of Young’s Modulus
M 60/40 panels have the highest Young’s Modulus
C 80/20 and R 80/20 panels have the lowest Young’s Modulus
In terms of acoustic isolation
In terms of thermal isolation
R 80/20 and T 60/40 panels provide the best thermal insulation
M 60/40 and OPEFB 50/50 panels are not thermal insulators
Higher fiber loading had no significant effect on absorbance
Cocoa has the highest absorption  Good for limiting echo and reverberation
Typha, Millet, and OPEFB have high transmission loss Good for soundproofing
Higher filler loading lowered the transmission loss values of rice and cocoa panels