## Slide 1
Valorization of Agricultural Residues or Wastes into Biochar for a Circular Economy
Presenters name(s):
Affiliation : INP-HB
B4A Final Conference/BLP 2025,
28-30 January, Montpellier

## Slide 2
PRODUCTION OF BIOCHAR
WATER FILTRATION
SOIL AMENDMENT

## Slide 3
Productor in the word of
Cocoa and cashew
Agriculture wastes materials

## Slide 4
Specifique Surface (m2/g) | total Volume of pores (cm3/g) | Mean dameter of pores(nm)
341,11 | 0,80 | 1,44
Elements | Values (%)
C | 76,65
O | 18,65
P | 0,26
K | 1,91
Ca | 0,30
Mg | 0,13
Si | 0,10
FTIR analysis
SEM analysis
Biochar
Raw materials
Traditionnel kiln
Bresilen kiln
Chemical analysis
BET analysis

## Slide 5
Water filtration
 | Before Trait. | After Trait. | Before Trait. | After Trait. | Normes OMS | 
pH | 6,69 | 6,4 | 6,63 | 6,3 | 6,5-8,5 | -
DCO | 610,1 | 10 | 518,4 | 13 | 30 | mg/L
AMMONIAQUE | 0,49 | 0,19 | 0,21 | 0,16 | 1,5 | mg/L
SULFATE | 33,6 | 20,76 | 36,54 | 25,85 | 250 | mg/L
CHLORURE | 60,35 | 21,3 | 49,7 | 24,85 | 200 | mg/L
MES | 56 | 0 | 62 | 0 | 25 | mg/L
NITRATE | 69,35 | 3,11 | 57,54 | 3,6 | 50 | mg/L
Filtration tests on the INP-HB experimental site have been completed
Rural area device in installed in the village of Dougba. Filtration tests will begin soon
Biochar
Sand
Sand
River
Treated water

## Slide 6
Biochar
SOIL AMENDMENT
Chart: Hauteur en cm
| 31 Jours | 41 Jours | 49 Jours | 57 Jours | 73 Jours | 89 Jours
2% biochar | 12.6667 | 16 | 23 | 32.6667 | 37.6667 | 63
5% biochar | 19.5 | 32.6667 | 49 | 72.3333 | 72.3333 | 179.3333
10% biochar | 6.3333 | 13 | 16.3333 | 29.6667 | 28.6667 | 44
Témoin | 12.8333 | 18 | 23.6667 | 34 | 34 | 50.3333
Tableau XII: Rendement moyen de tomate en grammes(g) |  |  |  | 
 | 0% biochar | 2% biochar | 5% biochar | 10% biochar
Sol-K | 700±0,2 | 2836,7±0,7 | 1856,7±0,2 | 316,7±0,6
Sol-D | 733,3±0,5 | 1866,7±1,3 | 1600±1;0 | 168,3±0,6
Sol-Y | 220,3±0,7 | 840±0,3 | 658,3±1,2 | 136,7±0,5
Biochar soil amendment trials
Biochar soil amendment trials in the farm
Evolution of the high of tomatos plants

## Slide 7
SOIL AMENDMENT
One pyrolysis kiln construction and Field soil amendment trials : to be implemented in cooperative Kapatchiva zone. Contract signed (see photos)

## Slide 8
Water filtration